Weld Map For Steel Structure

| Rev. PAGE No. | 00 | 01 | 02 | 03 | 04 | 05 | 06 | 07 | 08 | Rev. PAGE No. | 00 | 01 | 02 | 03 | 04 | 05 | 06 | 07 | 08 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | x |  |  |  |  |  |  |  |  | 36 |  |  |  |  |  |  |  |  |  |
| 2 | x |  |  |  |  |  |  |  |  | 37 |  |  |  |  |  |  |  |  |  |
| 3 | x |  |  |  |  |  |  |  |  | 38 |  |  |  |  |  |  |  |  |  |
| 4 | x |  |  |  |  |  |  |  |  | 39 |  |  |  |  |  |  |  |  |  |
| 5 | x |  |  |  |  |  |  |  |  | 40 |  |  |  |  |  |  |  |  |  |
| 6 | x |  |  |  |  |  |  |  |  | 41 |  |  |  |  |  |  |  |  |  |
| 7 |  |  |  |  |  |  |  |  |  | 42 |  |  |  |  |  |  |  |  |  |
| 8 |  |  |  |  |  |  |  |  |  | 43 |  |  |  |  |  |  |  |  |  |
| 9 |  |  |  |  |  |  |  |  |  | 44 |  |  |  |  |  |  |  |  |  |
| 10 |  |  |  |  |  |  |  |  |  | 45 |  |  |  |  |  |  |  |  |  |
| 11 |  |  |  |  |  |  |  |  |  | 46 |  |  |  |  |  |  |  |  |  |
| 12 |  |  |  |  |  |  |  |  |  | 47 |  |  |  |  |  |  |  |  |  |
| 13 |  |  |  |  |  |  |  |  |  | 48 |  |  |  |  |  |  |  |  |  |
| 14 |  |  |  |  |  |  |  |  |  | 49 |  |  |  |  |  |  |  |  |  |
| 15 |  |  |  |  |  |  |  |  |  | 50 |  |  |  |  |  |  |  |  |  |
| 16 |  |  |  |  |  |  |  |  |  | 51 |  |  |  |  |  |  |  |  |  |
| 17 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 19 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 20 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 21 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 23 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 24 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 25 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 26 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 27 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 28 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 29 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 30 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 31 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 32 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 33 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 34 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 35 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

| 2 | 1 | WELD DETAIL NO. |  |
| --- | --- | --- | --- |
|  |  | PREPARATION |  |
| ST 37-2 | ST 37-2 | MATERIAL GRADE |  |
| THK. > 16 mm | ALL | THICKNESS |  |
| GMAW | GMAW | WELD PROCESS |  |
| ROOT AND FILL | ROOT AND FILL | WELDING LAYER |  |
| AWS A5.18 ER 70S-6(1.2mm) | AWS A5.18 ER 70S-6(1.2mm) | WELDING CONSUMABLE |  |
| 220-268 | 190-220 | AMPERES | WELDING TECHNIQUE |
| 18-32 | 18-32 | VOLTS |  |
| 25-60 | 25-60 | TRAVEL SPEED(cm/min) |  |
| 780 | 750 | HEAT INPUT (j/mm) |  |
| DCEP | DCEP | POLARITY |  |
| 1G,2G,3G | 1F & 2F | POSITION |  |
| WP002 | WP001 | WPS |  |
| SSS-PQR002A | SSS-PQR001A | SUPPORTING PQR |  |
| Min 15°C For T≤38 & 65°C For 38<T≤65 | Min 10°C For T≤38 & 65°C For 38<T≤65 | MINIMUM PREHEAT TEMP. | HEAT TREATMENT |
| 65° C | 250° C | MAXIMUM PREHEAT TEMP. |  |
| 300° C | 300° C | MAXIMUM Inter Pass Temp. . |  |
| N.A | N.A | POST WELD HEAT TREATMENT |  |
| According to AWS D1.1 (2015) | According to AWS D1.1 (2015) | REMARK |  |

| 4 | 3 | WELD DETAIL NO. |  |
| --- | --- | --- | --- |
|  |  | PREPARATION |  |
| ST 37-2 | ST 37-2 | MATERIAL GRADE |  |
| 6mm ˂ THK. ≤ 16 mm | 6mm ˂ THK. ≤ 16 mm | THICKNESS |  |
| GMAW | GMAW | WELD PROCESS |  |
| ROOT AND FILL | ROOT AND FILL | WELDING LAYER |  |
| AWS A5.18 ER 70S-6(1.2mm) | AWS A5.18 ER 70S-6(1.2mm) | WELDING CONSUMABLE |  |
| 215-264 | 210-255 | AMPERES | WELDING TECHNIQUE |
| 18-32 | 18-32 | VOLTS |  |
| 25-60 | 25-60 | TRAVEL SPEED (cm/min) |  |
| 840 | 820 | HEAT INPUT (j/mm) |  |
| DCEP | DCEP | POLARITY |  |
| 1G , 2G , 3G | 1G , 2G , 3G | POSITION |  |
| WP004 | WP003 | WPS NO |  |
| SSS-PQR004A | SSS-PQR002A | SUPPORTING PQR |  |
| 10°C For T≤38 & 65°C For 38<T≤65 | 10°C For T≤38 & 65°C For 38<T≤65 | MINIMUM PREHEAT TEMP. | HEAT TREATMENT |
| 250° C | 250° C | MAXIMUM PREHEAT TEMP. |  |
| 300° C | 300° C | MAXIMUM Inter Pass Temp. |  |
| N.A | N.A | POST WELD HEAT TREATMENT |  |
| According to AWS D1.1 (2015) | According to AWS D1.1 (2015) | REMARK |  |

| 6 | 5 | WELD DETAIL NO. |  |
| --- | --- | --- | --- |
|  |  | PREPARATION |  |
| ST 37-2 | ST 37-2 | MATERIAL GRADE |  |
| THK. ≤ 6 mm | THK. > 16 mm | THICKNESS |  |
| GMAW | GMAW | WELD PROCESS |  |
| ROOT AND FILL | ROOT AND FILL | WELDING LAYER |  |
| AWS A5.18 ER 70S-6(1.2mm) | AWS A5.18 ER 70S-6(1.2mm) | WELDING CONSUMABLE |  |
| 210-280 | 220-268 | AMPERES | WELDING TECHNIQUE |
| 18-32 | 18-32 | VOLTS |  |
| 25-60 | 25-60 | TRAVEL SPEED (cm/min) |  |
| 780 | 780 | HEAT INPUT (j/mm) |  |
| DCEP | DCEP | POLARITY |  |
| 1G , 2G | 1G , 2G, 3G | POSITION |  |
| WP06 | WP05 | WPS |  |
| SSS-PQR003A | SSS-PQR004A | PQR |  |
| Min 10°C For T≤38 & 65°C For 38<T≤65 | Min 15°C For T≤38 & 65°C For 38<T≤65 | MINIMUM PREHEAT TEMP. | HEAT TREATMENT |
| 250° C | 250° C | MAXIMUM PREHEAT TEMP. |  |
| 300° C | 300° C | MAXIMUM Inter Pass Temp |  |
| N.A | N.A | POST WELD HEAT TREATMENT |  |
| According to AWS D1.1 (2015) | According to AWS D1.1 (2015) | REMARK |  |

| - | 7 | WELD DETAIL NO. |  |
| --- | --- | --- | --- |
|  |  | PREPARATION |  |
|  | ST 37-2 | MATERIAL GRADE |  |
|  | 10 < Thk. ≤ 40 | THICKNESS |  |
|  | SAW | WELD PROCESS |  |
|  | 1~n | WELDING LAYER |  |
|  | A-5.17 F7AZ-EM 12 | WELDING CONSUMABLE |  |
|  | 360-570 | AMPERES | WELDING TECHNIQUE |
|  | 28-35 | VOLTS |  |
|  | 20-40 | TRAVEL SPEED (cm/min) |  |
|  | 2852 | HEAT INPUT (j/mm) |  |
|  | DCEP | POLARITY |  |
|  | 1F | POSITION |  |
|  | WP007 | WPS |  |
|  | SSS- P.Q.R No.: 5329-2 | PQR |  |
|  | Min 10°C For T≤38 & 65°C | MINIMUM PREHEAT TEMP. | HEAT TREATMENT |
|  | 250° C | MAXIMUM PREHEAT TEMP. |  |
|  | 300° C | MAXIMUM Inter Pass Temp |  |
|  | N.A | POST WELD HEAT TREATMENT |  |
|  | According to AWS D1.1 (2015) | REMARK |  |