STYRENE PARK OFFSITE WPS

| R0 | 22-Dec.-2024 | IFA | F.Malekifar | M.Yasini | GH.Azizi |
| --- | --- | --- | --- | --- | --- |
| Rev. | Issued Date | DESCRIPTION | PREPARED | CHECKED | APPROVED |

REVISION RECORD SHEET

| Page Page | Revisions |  |  |  |  |  |  |  | Page | Revisions |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | R0 | R1 | R2 | R3 | R4 | R5 | R6 |  |  | R0 | R1 | R2 | R3 | R4 | R5 | R6 |
| 1 | X |  |  |  |  |  |  |  | 39 |  |  |  |  |  |  |  |
| 2 | X |  |  |  |  |  |  |  | 40 |  |  |  |  |  |  |  |
| 3 | X |  |  |  |  |  |  |  | 41 |  |  |  |  |  |  |  |
| 4 | X |  |  |  |  |  |  |  | 42 |  |  |  |  |  |  |  |
| 5 | X |  |  |  |  |  |  |  | 43 |  |  |  |  |  |  |  |
| 6 |  |  |  |  |  |  |  |  | 44 |  |  |  |  |  |  |  |
| 7 |  |  |  |  |  |  |  |  | 45 |  |  |  |  |  |  |  |
| 8 |  |  |  |  |  |  |  |  | 46 |  |  |  |  |  |  |  |
| 9 |  |  |  |  |  |  |  |  | 47 |  |  |  |  |  |  |  |
| 10 |  |  |  |  |  |  |  |  | 48 |  |  |  |  |  |  |  |
| 11 |  |  |  |  |  |  |  |  | 49 |  |  |  |  |  |  |  |
| 12 |  |  |  |  |  |  |  |  | 50 |  |  |  |  |  |  |  |
| 13 |  |  |  |  |  |  |  |  | 51 |  |  |  |  |  |  |  |
| 14 |  |  |  |  |  |  |  |  | 52 |  |  |  |  |  |  |  |
| 15 |  |  |  |  |  |  |  |  | 53 |  |  |  |  |  |  |  |
| 16 |  |  |  |  |  |  |  |  | 54 |  |  |  |  |  |  |  |
| 17 |  |  |  |  |  |  |  |  | 55 |  |  |  |  |  |  |  |
| 18 |  |  |  |  |  |  |  |  | 56 |  |  |  |  |  |  |  |
| 19 |  |  |  |  |  |  |  |  | 57 |  |  |  |  |  |  |  |
| 20 |  |  |  |  |  |  |  |  | 58 |  |  |  |  |  |  |  |
| 21 |  |  |  |  |  |  |  |  | 59 |  |  |  |  |  |  |  |
| 22 |  |  |  |  |  |  |  |  | 60 |  |  |  |  |  |  |  |
| 23 |  |  |  |  |  |  |  |  | 61 |  |  |  |  |  |  |  |
| 24 |  |  |  |  |  |  |  |  | 62 |  |  |  |  |  |  |  |
| 25 |  |  |  |  |  |  |  |  | 63 |  |  |  |  |  |  |  |
| 26 |  |  |  |  |  |  |  |  | 64 |  |  |  |  |  |  |  |
| 27 |  |  |  |  |  |  |  |  | 65 |  |  |  |  |  |  |  |
| 28 |  |  |  |  |  |  |  |  | 66 |  |  |  |  |  |  |  |
| 29 |  |  |  |  |  |  |  |  | 67 |  |  |  |  |  |  |  |
| 30 |  |  |  |  |  |  |  |  | 68 |  |  |  |  |  |  |  |
| 31 |  |  |  |  |  |  |  |  | 69 |  |  |  |  |  |  |  |
| 32 |  |  |  |  |  |  |  |  | 70 |  |  |  |  |  |  |  |
| 33 |  |  |  |  |  |  |  |  | 71 |  |  |  |  |  |  |  |
| 34 |  |  |  |  |  |  |  |  | 72 |  |  |  |  |  |  |  |
| 35 |  |  |  |  |  |  |  |  | 73 |  |  |  |  |  |  |  |
| 36 |  |  |  |  |  |  |  |  | 74 |  |  |  |  |  |  |  |
| 37 |  |  |  |  |  |  |  |  | 75 |  |  |  |  |  |  |  |
| 38 |  |  |  |  |  |  |  |  | 76 |  |  |  |  |  |  |  |

# PURPOSE

This document, apply to the preparation of Welding Procedure Specifications (WPS) for welding processes permitted in this Part. These rules are based on the welding general requirements of ASME Sec. IX and Sec. V .

# Abbreviations

WPS: WELDING PROCEDURE SPECIFICATION

# project definitions

| Abbr. | Description |
| --- | --- |
| PROJECT | Structure Fabrication of Chiller Skid |
| OWNER | Polymer Pad Jam Co |
| MC | Toase-ehe Park Sanati Gohar Ofogh |
| CONTRACTOR | HSE |
| Vendor | # Arkan Sanat Paydar Company(ASP) |

| WELDING PROCEDURE SPECIFICATION ( WPS ) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | DOC. NO.: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OWNER: |  |  |  |  |  |  | WPS NO. : 01 |  |  |  |  |  |  |  |  | WELDING PROCESS : SMAW |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | STANDARD: ASME IX 1998 |  |  |  |
| CONTRACTOR: |  |  |  |  |  |  | SUPPORTING PQR NO: |  |  |  |  |  |  |  |  |  |  |  |  |  | Rev:00 |  |  |  |  |  | DATE: |  |  |  |  |  |  |  |  |  |
| JOINTS ( QW – 402 ) Joint Desigen : Fillet weld Backing : Yes No Backing Material : Base metal |  |  |  |  |  |  |  |  |  | Detail: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| BASE METALS( QW – 403 ) P-NO. : 1 Group-No. :1 TO P-No. : 1 Group-No. : 1 Specification Type & Grade : SA-36 to SA-36 Thickness Range (Groove or Fillet ) :5 ~20 Pipe Diameter Range (Groove or Fillet ): NA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | FILLER METALS(QW – 404) Spec. No. (SFA): 5.1 Aws . No. (Class) : E7018 AMA F. No. : 4 A.No. : 1 Flux Type (Classification) : NA Note: The Drying and Holdling Conditions shall be according to the manufacturer’s recommendations. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| POSITONS ( QW- 405 ) Position(s) Of (Groove or Fillet ) : ALL Welding Progression : Up Ward or Down Ward |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | GAS(QW-408); Gas(es); Percent Composition; Flow Rate(l/m). Shielding; -; -; -. Trailing; -; -; -. Backing; -; -; -. |
| TECHNIQUE ( QW – 410 ) String Or Weave Bead : String or Weave Orifice Or Gas Cup Size : 12mm Initial & Inter Pass Cleaning : Brushing Method Of Back Gouging : NA Single or Multiple Electrode : Single |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ELECTERICAL CHARACTERISTICS (QW-409) Other : refer to welding sequence table |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREHEAT ( QW- 406 ) Preheat Temp. : NA Inter Pass Temp. : Max 205 ºC Preheat Maintenance: NA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | POSTWELD HEAT TREATMENT(QW-407) Temperature Range : NA Heating rate : NA Cooling rate : NA Hold Time : NA |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDING SEQUENCE |  | Weld Layer(es) |  | WeldingType |  |  |  | Welding Proccess |  |  | FillerMetal |  |  |  |  |  |  | Current |  |  |  |  |  |  |  |  |  |  |  |  | Travel Speed Range ( Cm/ min) |  |  |  | Other |  |
|  |  |  |  |  |  |  |  |  |  |  | Class |  | Dia. |  |  |  |  | Type& Polar. |  |  |  |  |  |  | Amp. Range |  |  |  | Volt. Range |  |  |  |  |  |  |  |
|  |  | 1 – n |  | Manual |  |  |  | SMAW |  |  | E7018 |  | 3.2/4 |  |  |  |  | DCEP |  |  |  |  |  |  | 70-120 |  |  |  | 20-26 |  | 20-25 |  |  |  |  |  |
| WELDING PROCEDURE SPECIFICATION ( WPS ) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | DOC. NO.: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| OWNER: |  |  |  |  |  | WPS NO. : 02 |  |  |  |  |  |  |  |  | WELDING PROCESS : SMAW |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | STANDARD: ASME IX 1998 |  |  |  |
| CONTRACTOR: |  |  |  |  |  | SUPPORTING PQR NO: |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Rev:00 |  |  |  |  |  | DATE: |  |  |  |  |  |  |  |  |  |
| JOINTS ( QW – 402 ) Joint Desigen : Groove weld Backing : Yes No Backing Material : NA |  |  |  |  |  |  |  |  |  | Detail: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| BASE METALS( QW – 403 ) P-NO. : 1 Group-No. :1 TO P-No. : 1 Group-No. : 1 Specification Type & Grade : SA-36 to SA-36 Thickness Range (Groove or Fillet ) :5 ~20 Pipe Diameter Range (Groove or Fillet ): NA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | FILLER METALS(QW – 404) Spec. No. (SFA): 5.1 Aws . No. (Class) : E7018 AMA F. No. : 4 A.No. : 1 Flux Type (Classification) : NA Note: The Drying and Holdling Conditions shall be according to the manufacturer’s recommendations. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| POSITONS ( QW- 405 ) Position(s) Of (Groove or Fillet ) : ALL Welding Progression : Up Ward or Down Ward |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | GAS(QW-408); Gas(es); Percent Composition; Flow Rate(l/m). Shielding; -; -; -. Trailing; -; -; -. Backing; -; -; -. |
| TECHNIQUE ( QW – 410 ) String Or Weave Bead : String or Weave Orifice Or Gas Cup Size : 12mm Initial & Inter Pass Cleaning : Brushing Method Of Back Gouging : NA Single or Multiple Electrode : Single |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ELECTERICAL CHARACTERISTICS (QW-409) Other : refer to welding sequence table |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREHEAT ( QW- 406 ) Preheat Temp. : NA Inter Pass Temp. : Max 205 ºC Preheat Maintenance: NA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | POSTWELD HEAT TREATMENT(QW-407) Temperature Range : NA Heating rate : NA Cooling rate : NA Hold Time : NA |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDING SEQUENCE |  | Weld Layer(es) |  | WeldingType |  |  | Welding Proccess |  |  |  | FillerMetal |  |  |  |  | Current |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Travel Speed Range ( Cm/ min) |  |  |  | Other |  |
|  |  |  |  |  |  |  |  |  |  |  | Class |  | Dia. |  |  | Type& Polar. |  |  |  |  |  |  |  |  | Amp. Range |  |  |  | Volt. Range |  |  |  |  |  |  |  |
|  |  | 1 – n |  | Manual |  |  | SMAW |  |  |  | E7018 |  | 3.2/4 |  |  | DCEP |  |  |  |  |  |  |  |  | 70-120 |  |  |  | 20-26 |  | 20-25 |  |  |  |  |  |